## Slide 1
Photovoltaics:
Fundamental concepts and novel systems
First practical photovoltaic cell:
Chapin, Fuller, Pearson,
Bell Labs, 1954: 6% efficiency
THANKS TO
GARY H O D E S
& many others
Notes: 1

## Slide 2
Outline
Energy levels  bands
Doping of semiconductors
Energy band alignments between different phases
Space charge layers
p-n junctions, Schottky barriers
p-n cells, Si cells, thin film cells
Schottky cells (solid and liquid junction)
p-i-n cells
Fundamental limits of photovoltaic cells
How to overcome/ bypass these limits
New generation cells (brief survey)
PV stability, efficiencies and economics
Notes: 1 (2)

## Slide 3
From energy levels to bands
E
If EG < ~100-150x kTB
 semiconductor
1 e- energy
EG
EV
EC
CB
VB
HOMO
LUMO
Notes: 4 (8)

## Slide 4
Doping of semiconductors
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
As
B C N
Al Si P
Ga Ge As
EC
E
EV
EG 1.1 eV
n-type
As5+ ---> 4e-+ e- donors (ND)
EF = Fermi level (~electrochemical
potential of electrons
+ + + + + + + + + + + +
          
Free electrons in CB

## Slide 5
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
B C N
Al Si P
Ga Ge As
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
B
1018
1016
DE = kTln(ND/NC)
0 or
ND=NA
1010
1 e- energy
Doping of semiconductors -2
p-type
B3+ ---> 3e- - e-
Acceptors (NA)
EC
EV
EF
        
Free holes
in VB
Notes: 7 (15)

## Slide 6
Energy band alignments between different phases
n-type
semiconductor
Evac
metal
EF
work function
electron affinity
e-
space charge
layer
Formation of a metal - semiconductor junction
n-type
p-type
space charge layer
 Formation of a p-n homojunction
1 e- energy
1 e- energy
space coordinate
Notes: 4 (19)

## Slide 7
Space Charge layers
Width of space charge layer inversely proportional
to [doping density]1/2
2ee0V
qND(A)
1/2
W =
Typical widths of space charge layer:
N = 1022/cc (metallic) Ångstroms (~ 1-2 atomic layers)
N = 1018/cc (heavily doped semiconductor) 10s of nm
N = 1016/cc (medium doped semiconductor) 100s of nm
N = 1014/cc (low doped semiconductor) few µm
In a photovoltaic cell, the width of the space charge layer should be wide enough
to absorb most of the light in the E-field region –a few 100 nm in a typical cell.
Light absorption I = I0e-ad
space charge
layer
Notes: 2 (21)

## Slide 8
Basics of photovoltaic cells
EC
EV
EF
e-
h+
hn
Charge separation in energy
Charge separation in space
e-
hn
h+
space coordinate
1 e- energy
1 e- energy

## Slide 9
e-
hn
h+
Amps
@ short circuit
VOC
Volts
@ open-circuit
V
load
@maximum power
Basics of photovoltaic cells

## Slide 10
ISC
VOC
max power
fill factor = (I mp . Vmp) / (I SC . VOC)
mp : max power
Voltage
Current
Dark- and Photo- I-V (current-voltage)
characteristics of a PV cell
Notes: 8 (29)

## Slide 11
Other ways of creating a built-in field to separate charges
p-n heterojunction
CdTe/CdS
CdS
CdTe
back contact (Cu/Cu2Te)
TCO front contact
CdTe
CdS
e-
h+
Silicon
homojunction

## Slide 12
Ginley, Collins & Cahen in Ginley & Cahen,
Fundamentals of Materials for Energy…
space
1 e- energy
Absorb light
Absorbed light creates carriers
Carrier collection, by diffusion, drift
Summary of how p-n junction PV cell works

## Slide 13
n-type
semiconductor
E0
metal
EF
work function
electron affinity
space charge
layer
Metal-semiconductor junction
(with semiconductor/ liquid electrolyte junction 
photoelectrochemical cell [PEC], where EF ≅ ERedox
Other ways of creating a built-in field to separate charges -2

## Slide 14
p-i-n (I = insulator) cell
EO
EC
EV
N = 1018/cc (heavily doped semiconductor) 10s of nm
N = 1016/cc (medium doped semiconductor) 100s of nm
N = 1014/cc (low doped semiconductor) few µm
Reminder of
typical space charge layer widths
Other ways of creating a built-in field to separate charges -3
Notes: 6 (35)

## Slide 15
Chapin
Fuller
Pearson
1954
2014

## Slide 16
Si (crystalline) cells : 1st generation cells
(thin film) CdTe, CIGS, α-Si : 2nd generation cells
Dye cells, organic cells and related ones : 3rd generation cells
There are newer ones and ‘generation number’ becomes fuzzy at this stage
Solar cell generations
Notes: 1 (44)

## Slide 17
Organic
CdTe
GaAs
“the single crystal divide”

## Slide 18
one electron energy
space
Generalized picture
Metastable high and low energy states
Absorber transfers charges into high and low energy state
Driving force brings charges to contacts
Selective contacts
    (1) cf. e.g., Green, M.A., Photovoltaic principles. Physica E, 14 (2002) 11-17
The Photovoltaic (PV) effect:
High
energy
state
Low
energy
state
Absorber
e-
p+
contact
contact
Notes: 2 (4)

## Slide 19: Fundamental losses in single junction solar cell
e
-
-
voltage (
qV
)
e
-
n
-
type
p
-
type
h
n
h
+
e
-
useable photo
-
voltage (
qV
)
Energy
e
-
n
-
type
p
-
type
h
n
h
+
O. Niitsoo
space
high energy photon – partial loss
low energy photon – total loss

## Slide 20
>Eg
thermalized
< Eg
not absorbed
Etendu; Photon entropy –TD
~0.3eV @RT, lack of concentration
Carnot factor –TD
Emission loss- (current)
Electrical power out
Current – Voltage Characteristics
After Hirst & Ekins-Daukes
Prog.Photovolt:Res:Appl. (2010)
All fundamental losses in PV cell
Eg
Nayak, ……, Cahen., Energy Environ. Sci., 2012

## Slide 21: Shockley-Queisser* (SQ) Limit
detailed balance,
photons-in = electrons-out + photons-out;
on earth, @ RT,
for single absorber / junction;
cf. also Duysens (1958) “The path of light in photosynthesis”; Brookhaven Symp. Biol.
Prince, JAP 26 (1955) 534
Loferski, JAP 27 (1956) 777
Shockley & Queisser JAP (1961)

## Slide 22: How to circumvent SQ and other losses?
Better utilization of sunlight: Photon management:
Multi-bandgap, multi-junction photovoltaics
GaInP2 Eg = 1.8-1.9 eV up to 1.45 V VOC
Notes: 8 (43)

## Slide 23: Up-conversion for a single junction
2 photons of energy 0.5 Eg< hν< Eg
are converted to 1 photon of hν> Eg
How to circumvent these losses?

## Slide 24: Down-conversion for a single junction
1 photon of energy hν > 2Eg
is converted into 2 photons of hν > Eg
How to circumvent these losses?

## Slide 25: Other ways to beat the SQ limit
e-
h+
e-
e-
h+
h+
Multiple exciton generation
Hot electrons
Intermediate bandgap
EG
EV
EC
EC*

## Slide 26
e-
h+
Multiple exciton generation
Hot electrons
Intermediate bandgap
EG
EV
EC
EC*
e-
EF
EF
Other ways to beat the SQ limit

## Slide 27: Other ways to beat the SQ limit
e-
h+
Multiple exciton generation
Hot electrons
Intermediate bandgap
EG
EV
Ei
EC
e-
Notes: 4 (for 3 slides) (71.5)

## Slide 28: The principle of nanostructured cells
contact
contact
electron conductor hole conductor
absorber
light absorption
depth
e-
h+
light-absorbing
semiconductor
e-
h+
Advantage of high surface area: Allows the use of locally thin absorber and therefore poor quality
(wider range of) absorbers
e-
h+
hole
selective
contact
electron
selective
contact
EC
EV
electron (hole) selective contact; conductor; transport medium
Notes: 4 (48)

## Slide 29
Organic photovoltaic cells OPV
Two problems of OPV:
Low diffusion lengths of electron/hole
2. Low dielectric constant – high binding energy
e-
h+

## Slide 30
e-
h+
Wannier-Mott excitons – extended; low BE few/tens meV
Frenkel excitons – localized; high BE hundreds meV
Binding energy of H atom =
me4
2h2ε2
= 13.6 eV
e-
e-
h+
h+
e-
e-
h+
Two problems of OPV:
Low diffusion lengths of electron/hole
2. Low dielectric constant and high effective mass – high binding energy
Binding energy of exciton ?
effective mass of
electrons and holes
dielectric constant
of material

## Slide 31
Notwithstanding these problems, OPV is now at ~ 11% conversion efficiency
Stability still not good enough for practical use, but improving
Advantages: Cheap (in capital and in energy)
Roll-to-roll manufacturing (large scale possible)
Notes: 8 (56)

## Slide 32
Dye sensitized solar cell (DSC or DSSC)
HOMO
LUMO
e-
e-
h+
light
e-
I- + h+ ---> I
2I + I- ---> I3- (I is soluble in I-)
At counter electrode, I is reduced back to I-
Important difference between this cell and “standard’ photovoltaic cells
or previous nanocrystalline cell:
Charge generation and charge separation occur in different phases:
recombination is inherently low.
semiconductor
dye
TiO2
EC
EV
TiO2
Need single monolayer
dye on TiO2
But then low absorption

## Slide 33
Solution - use high surface area semiconductor
Early attempts increased surface area by roughening electrode - several times increase
Breakthrough: porous, nanocrystalline TiO2
Made by sintering a colloid or suspension of TiO2
O’Regan, B.; Grätzel, M. Nature 1991, 353, 737.
Dye molecule bonded to TiO2
Only a monolayer of dye at most on each TiO2

## Slide 34
The most common dye: Ru(dcbpyH2)2(NCS)2 or RuL2(NCS)2
cis-bis(4,4’-dicarboxy-2,2’-bipyridine)-bis(isothiocyanato)ruthenium(II)
Ti
N
Ru
N
C
-O
O
C
-O
O
e-
Excitation of dye is a metal-to-ligand
charge transfer
Ru d-orbitals
ligand p* orbital
Ti4+/3+
ca. 1.7 eV
N=C=S
N=C=S
h+
Notes: DSC 5 (61)

## Slide 35
Change the dye in a DSC to a semiconductor
Semiconductor-sensitized solar cells (quantum dot cells)
ETA (extremely thin absorber) solar cells
Variations:
Hole conductor – liquid or solid (if solid, commonly called ETA cell)
Semiconductor may be in the form of quantum dots – increase in Eg
Semiconductor does not have to be a single monolayer – typically few nm to few tens nm
Notes: 2.5 (63.5)

## Slide 36
Hybrid Organic-Inorganic Perovskites
most common one- CH3NH3PbI3
Preparation
CH3NH2+HI  CH3NH3I(solid) in methanol, at 0˚C
CH3NH3X + PbI2  CH3NH3PbI3 in organic solvent
Solution processable, easy to scale
Heat at ca. 100ºC
Another +: very high VOC for CH3NH3PbI3 EG = 1.55 eV, VOC up to 1.2 V
Notes: 4 (67.5)

## Slide 37
Evolution of hybrid I-O perovskite
solar cells

## Slide 38
The three important parameters for commercial cells
1. Efficiency

## Slide 39:  Shockley-Queisser* (SQ) Limit

## Slide 40
2. Stability Long term stability of PV modules/systems
Jordan & Kurtz, 2011 (August), National Renewable Energy
Laboratory (NREL)
Photovoltaic degradation rates – An analytical review
<2000 >2000 <2000 >2000 <2000 >2000 <2000 >2000 <2000 >2000
mean

## Slide 41
3. Cost (money and energy)
$/WP
Energy payback time
$0.6/WP in 2030
Predicted cost

## Slide 42
(US)

## Slide 43
Solar PV Costs in the USA and Germany (2013)
A C O L D S H O W E R

## Slide 44
from
First Solar
website…
Peng, Lu, Yang,
Renew. Sustain. Energy Rev.
19 (2013) 255–274
Estimated Solar Cell Energy Payback Times 2013

## Slide 45
Wikipedia
And finally, PV production history and forecast
Cumulative PV
Notes: 10 (81.5)

## Slide 46
World’s Largest Solar-Electric Plant
30 TWp (~ 6 TWC)
requires 1 such plant,
every HOUR, for
~ 12 years (+ storage…)
Solar Cell Power Stations TODAY
In 12/2014 Global Cumulative Installed PV Power ~ 0.15 TWp
PRC goal >2012
≥ 0.01 TWp/yr
0.55 GWp ( ~100 MWc) Topaz Solar farm (CA, USA)
Notes: PRC 2011 2 GWp solar (PV)