## Slide 1: c-Si/PEDOT:PSS Interface Modification a Model for Studying Hybrid Organic-Inorganic Systems
Ann Ericksson, Arava Zohar, Nir Kedem
Thanks also to
Ayelet Vilan; Rotem Har-Lavan; Igor Lubomirsky & David Ehre (C-V);
Rafi Kalish - Technion (H-plasma); Lars Korte – HBZ
$ €: Helmsley trust
Minerva foundation
Int’l. Mini-Symposium on Organic Semiconductors:
Their Electronic Structures and Device Physics
Chiba , Jan. 28, 2015

## Slide 2: Motivation
Explore use of “inversion layer” PV* device
by controlling interface properties of Si in MIS** cell,
using monomolecular layers on Si
* PhotoVoltaic **Metal-Insulator-Semiconductor

## Slide 3: Metal-Semiconductor (MS) junction
EG
Metal
1
Semi-
conductor
EF
Accumulation
Depletion
EG
Metal
2
Semi-
conductor
EF
MAJORITY carrier
Inversion
Metal
3
Semi-
conductor
EF
EG
MINORITY carrier

## Slide 4: Inversion layer device Metal-Semiconductor (MS) junction
based on Schottky-Mott model
BH
BH

## Slide 5
By adding insulating layer to MS junction we can passivate the Si surface and tune Si Electron Affinity (χs)
n- type
P
t ype
Inversion layer device From MS to MIS junction

## Slide 6: Questions
(How) can a molecular monolayer control the electronic properties of an (MIS) junction
Is surface dipole retained if interface forms?
To what extent can this affect PV device performance?
Can mc-Si surface be passivated and modified by ultra-thin (< 2 nm) molecular monolayer?

## Slide 7: Experimental system
mc n-Si
Organic monolayer
PEDOT:PSS
sc n-Si
Eutectic InGa
Multi-crystalline (mc) Si
Rough surface (few μm)
<111>, <110>, <311>, <331> mixed orientation
Single crystalline (sc) Si
Flat surface (< nm roughness)
<111> or <100> orientation.
A.-E. Haj-Yahia, et al. Adv. Mater., 2013, 25,702–706
R. Har-Lavan, et al. J. Appl. Phys., 2013, 113, 084909
Modified surface
Me- styrene
Br- styrene
Ethynyl Toluene
Butoxy
Methoxy
M
I
S
Br
CH3
CH3

## Slide 8: Work function (WF) modification
Single Crystal (sc) and multi-crystalline (mc) n-Si WF modification measured by CPD
~ 800mV
~ 600mV
~ 850mV
~ 1000mV
Si WF modification > 0.7 V…  inversion?

## Slide 9: Inversion requires well-passivated interface  Silicon passivation
Sample | Minority carrier lifetime sc-Si[μsec] | SPV sc-Si [mV] | SPV mc-Si [mV]
H-terminated <111> | 42 | 80 | 90
Br-styrene <111> | - | 105 | 65
Me-styrene <111> | 20 | 165 | 85
ET <111> | 18 | 235 | 105
Methoxy +HQ <100> | 28 | 292 | 162
SiO2 <111> | 8 | 210 | 150
Minority Carrier Lifetime
Molecules can passivate mc-Si
Surface Photo-Voltage, SPV


## Slide 10
Passivation:
Surface Interface
mc n-Si
Organic monolayer
sc n-Si
contact
Eutectic InGa
M
I
S
? ?

## Slide 11: Molecular effect at sc-Si MIS with M=Hg
sc-Si / MML/ Hg (MML= mol. monolayer)
Molecules can tune junction behavior!!! (with M=Hg)
A.-E. Haj-Yahya et al., Adv,. Mater. 2013

## Slide 12: mc n-Si passivation
n-Si / Me-styrene/ Hg
Molecules can passivate mc-Si

## Slide 13: Molecular effect at mc-Si MIS with M=Hg
mc-Si / MML/ Hg
Molecules can passivate mc-Si,
but …
we cannot (YET) tune the interface

## Slide 14: CONTACTING Molecularly passivated surface  soft contact
Transparent in the visible and IR range (T > 90%)
High (5 eV) WF  invert n-Si?
Highly conductive (300-850 S/cm)
Deposit by soft methods such as spin coating or….
mc n-Si
sc n-Si
PEDOT:PSS
Organic monolayer
poly(3,4-ethylenedioxythiophene)
and poly(styrenesulfonate) (PEDOT:PSS)

## Slide 15: Lift-Off Float-On
PEDOT:PSS deposition by LOFO
  PEDOT:PSS layer deposited and annealed on sacrificial substrate, then floated onto device
  Avoids heating of device or exposing it to acidic solution
Deposit and anneal
PEDOT:PSS solution.
Partially dissolve substrate.
Float PEDOT onto H2O.
Lift substrate onto film, pump under vacuum.

## Slide 16: Energy band diagrams for inverted (a) and defect (b) interfaces
Notes: Energy band diagram for (a) an inversion layer formed between PEDOT:PSS and n-Si,
and (b) the energy band alignment that results with a significant number of defects
at the Si – contact interface.

## Slide 17: Barrier Height at MIS
 | BH [±0.03V] From J-V | SBH [±0.01V] n –Si/ PEDOT:PSS THEORETICAL SBH= Vbi + ζ * | 
sc-Si <111> / Me styrene | 0.89 | 0.98 | 
sc-Si <111> / ET | 0.83 | 0.98 | 
sc-Si <100> /Methoxy |  | 0.98 | 
sc-Si <111> /H | 0.84 | 0.98 | 0.88 NSLewis et al
Capacitance – Voltage
J-V data – Thermionic Emission
EC
Ef
EV
Eg=1.12eV

## Slide 18: Barrier Height at MIS
 | BH [±0.03V] From J-V | SBH [±0.01V] n –Si/ PEDOT:PSS theoretical value SBH= Vbi + ζ * | BH [±0.01V] From C-V
sc-Si <111> / Me styrene | 0.89 | 0.98 | 0.96
sc-Si <111> / ET | 0.83 | 0.98 | 0.98
sc-Si <100> /Methoxy | 0.86 | 0.98 | 0.90
sc-Si <111> /H | 0.84 | 0.98 | 0.91
Eg=1.12eV
EC
Ef
EV
J-V data – Thermionic Emission
C-V data –capacitance of inversion layer
EC
Ef
EV
Eg=1.12eV

## Slide 19: Advantages of C-V measurement
  Built-in voltage, depletion region width
  Semiconductor carrier density
  Density of interface defects
EC
Ef
EV
E
X
Si
Metal
Insulator
Vbi
W
Ec-Ef

## Slide 20: Equivalent circuits
C
R
n-Si/MML/PEDOT:PSS

## Slide 21: Equivalent circuits
Evac
Vbi
fb
n-Si
EF
IL
PEDOT: PSS
fm = 5.0 eV
CIL
RIL
n-Si/MML/PEDOT:PSS

## Slide 22: Built-in voltage (Vbi) from C-V @high ω
Notes: Results of C(V) measurements for samples with different ND, shown as A2/C2 vs V.
The inset shows data for the highest doping sample, which are displayed on a different scale.
Each curve represents an average of 3 devices.

## Slide 23: Built-in voltage (Vbi) from C-V @high ω
Slope ND
Intercept with X-axis VFB
B.Fabre C-V for n-Si –C18- Hg

## Slide 24
Built-in voltage, Vbi, vs. ND
A. Erickson et al. Adv. En. Mater. 2014

## Slide 25
Dark I-V curves for devices that were also measured by C(V).
Each curve is average of 2 (ND = 8.9x1016 cm-3) or 3(all other) devices.
A. Erickson et al. Adv. En. Mater. 2014
Barrier Height, φB, vs. ND

## Slide 26: J-V vs. C-V data
Different model system- coverage effect
Different bias regime (depletion vs. inversion)
Forward bias
Reverse bias

## Slide 27: Effect of n-Si Doping Density
ϕB from fits to the linear ln(J) - V region; Vbi extracted from C(V); Theory: ϕB = Vbi + |Ec - EF|.
Errors are standard deviations of fits to each individual sample.
A. Erickson et al. Adv. En. Mater. 2014

## Slide 28: MIS junction modification with M=PEDOT:PSS
n-type Si <111>
p-type IL
PEDOT:PSS
H
n-type Si <100>
p-type IL
PEDOT:PSS
H
H
MIS junction can reach theoretical limit

## Slide 29: Si-Organic Schottky solar cells (cf. R. Har-Lavan, D. Cahen, “40 yr of inversion PV”, IEEE J. PV (2013)
Use high work function transparent organic as top contact to n-Si  strong inversion
  PEDOT:PSS, PANI, or P3HT
  Can be applied to variety of Si surface morphologies
Q. Liu, et al. APL . 100, 183901 (2012).
~12 % @ IEEE PVSC 6-2013 Nagamatsu ….. Sturm
Influence of PEDOT:PSS composition
h = 11.3%
With 0.1% zonyl
Influence of Si morphology: nanocones
h = 11.1%
S. Jeong, et al. Nano Lett. 12, 2971 (2012).

## Slide 30
PEDOT:PSS contacts to Al2O3 inversion layer devices
  Strong inversion layer by oxide interface charges, contact via PEDOT:PSS
  Soft PEDOT:PSS deposition compatible with inversion-inducing molecular dipole layer
Interface dipole effect
PEDOT:PSS
-
-
-
-
-
-
-
-
-
-
-
-
-
-
+
+
+
+
+
+
+
+
+
n-type Si
+
+
+
+
+
Oxide charge
Inversion layer
H or Me-styrene passivation
h = 8.4%
1014 cm-3
Erickson et al.,APL 101, 233901 (2012);
Si-Organic INVERSION solar cells

## Slide 31
PEDOT:PSS – n-Si solar cell under 1 sun illumination
Voc = 0.56(1) V Jsc = 26.1(5) mA cm-2 η = 10.4(3)%
Si-Organic INVERSION solar cells

## Slide 32
Voc = 0.58 V
Isc = 32 mA/cm2
FF = 65 %
η ≥ 12%
Me styrene and Si- H
Br styrene
double diode
sc-Si /MML / PEDOT:PSS
Si-H/ PEDOT:PSS PV devices as good as best
Si-MML/ PEDOT:PSS ones (but less stable…)
Si-Organic INVERSION solar cells

## Slide 33: Conclusions
Characterization of energy band alignment @MIS interface is essential for electronic properties analysis.
  BH measured by C-V can highlight molecular effect.
Si <111> /MML / PEDOT:PSS interface presents maximum inversion(EV=EF).
For Si <100> interface only strong inversion reached .
  Surface reactivity can play important role for MIS junction
Inversion Si PV device reaches 12.5% solar to electrical conversion
mc-Si WF can be modified by molecular monolayer.
but as yet no WF tuning @MIS interface;  challenge for future
  mixed orientation and rough surface of mc-Si can result in low coverage.

## Slide 34
Results of measurements on transistor test devices, used to determine mobility in the
channel under the Al2O3 gate dielectric. Isd is shown as a function of Vsd, for different values
of Vg. Leakage current has been subtracted uniformly.
The inset shows a schematic of the device, where source, gate, and drain electrodes,
shown in blue, are all PEDOT:PSS.