## Slide 1: Noble (liquid) Dreams
Amos Breskin
Weizmann Institute of Science

## Slide 2: Noble (liquid) Dreams
Amos Breskin
Weizmann Institute of Science
Detection solutions for LARGE-VOLUME noble-liquid detectors

## Slide 3: The reality

## Slide 4
A two-phase TPC. WIMPs interact with noble liquid; primary scintillation (S1) is detected by bottom PMTs immersed in liquid. Ionization-electrons from the liquid are extracted under electric fields (Ed, and Eg) into the saturated-vapor above liquid; they induce electroluminescence in the gas phase – detected with the top PMTs (S2). The ratio S2/S1 provides means for discriminating gamma background from WIMPs recoils, due to the different scintillation-to-ionization ratio of nuclear and electronic recoils.
CLASSICAL DUAL-PHASE NOBLE-LIQUID TPC
Present:
XENON100, ZEPLIN, LUX….
Under design:
XENON1ton
Future:
MULTI-TON (e.g. Darwin):
COST
STABILITY
THRESHOLD

## Slide 5: Dual-phase TPC with GPM* S2 sensor
A proposed concept of a dual-phase DM detector. A large-area Gaseous Photo-Multiplier (GPM) (operated with a counting gas) is located in the saturated gas-phase of the TPC; it records, through a UV-window, and localizes the copious electroluminescence S2 photons induced by the drifting ionization electrons extracted from liquid. In this concept, the feeble primary scintillation S1 signals are preferably measured with vacuum-PMTs immersed in LXe. Under advanced R&D at WIS.
*GPM: Gaseous Photomultiplier
GPM

## Slide 6: Why Gaseous Photomultipliers?
Cost effective coverage of large areas
QEeff ~20% @ 175 nm with high filling factor
Can be of low radioactivity
Flat, thin geometry
Pixelated readout
May allow 4π coverage
Basic technology well understood and mastered
QE >30% @ 175 nm
(QEeff < 20% ; low fill factor)
Low radioactivity
Off-the-shelf
Years of proven operation
… But:
~M$/m2
Limited filling factor
Pixel size = PMT diameter
Present day PMTs for DM searches
Cryogenic GPMs for future large-scale DM searches

## Slide 7
Example: a triple-THGEM GPM
UV window (quartz)
mesh
CsI photocathode
Pixilated readout
Gas: Ne/CF4 or Ne/CH4
~10 mm
V1top
V1bot
V2top
V2bot
V3top
V3bot
most negative HV
ground

## Slide 8: The Thick Gas Electron Multiplier (THGEM)
Chechik 2004
Thickness 0.5-1mm
drilled
etched
SIMPLE, ROBUST, LARGE-AREA
Printed-circuit technology
(Also of radio-clean materials)
Double-THGEM: 10-100 higher gains
Robust, if discharge no damage
Effective single-electron detection
Few-ns RMS time resolution
Sub-mm position resolution
>MHz/mm2 rate capability
Cryogenic operation: OK
Broad pressure range: 1mbar - few bar
THGEM
0.5 mm
1e- in
104- 105 e-s out
E
ΔVTHGEM

## Slide 9: LXe-TPC/GPM
Nantes/Weizmann
171K
RT
107
104
1-THGEM
171K
Duval 2011 JINST 6 P04007
173K, 1100mbar

## Slide 10
GPM test setup
UV window
LXe
GPM (cascaded-THGEM) with pixelated readout
PMT
cathode
gate
anode
Operational Feb 2013

## Slide 11: Towards single-phase TPCs?
Simpler techniques?
Sufficient signals?
Lower thresholds?
Cheaper?
How to record best scintillation & ionization S1, S2?

## Slide 12: Single-phase spherical L-TPC
Central ball 4p covered with charge collecting and amplifying micro-structure (e.g. GEM)
in liquid phase
Sensitivity to single electron
High readout segmentation for
position information
Requirements:
CsI Photocathode
P. Majewski, LNGS 2006
S1: photoelectrons from CsI
S2: ionization electrons
S1, S2 electrons multiplied at the central ball
Feedback occurs as well
LXe
LXe
Idea: amplification in liquid phase
GEM
Unknown status

## Slide 13: Two-phase LXe/CsI: QE of CsI in LXe
Performance of Dual Phase XeTPC with CsI Photocathode and PMTs readout for the Scintillation Light
E. Aprile, K.L. Giboni, S. Kamat, P. Majewski, K. Ni, B.K. Singh and M. Yamashita. IEEE ICDL 2005, p345
CsI
S1
S4 photon-feedback
can be suppressed
by field gating
e-
e-
e-
PMTs
CsI
S2
S3
E
E
QE~25%
LXe-immersed CsI
Idea not yet materialized

## Slide 14: Single-phase option for PANDA
Karl Giboni
KEK Seminar Nov 2011
photosensors
photosensors
A
A
A
A
A
A
C
C
C
C
Anode-wire planes: S1 & S2
GPM
4p geometry with
immersed GPMs
LXe level
Demo facility in course

## Slide 15: LXe: some relevant numbers
Saturation of e- drift velocity: ~2.6 mm/ms @ 3 kV/cm
Threshold field for proportional scintillation: ~400 kV/cm
Threshold field for avalanche multiplication: ~1 MV/cm
Doke NIM 1982
Maximum charge gain measured 200-400 on:
wires, strips, spikes…
& LAr:
~500 UV photons/e- over 4p
measured with gAPD/WLS in
THGEM holes in LAr
Lightfoot, JINST 2009
THGEM holes in LAr

## Slide 16
The 70ties: Charge gain & Light yield in wires/LXe
Masuda NIM 1979
LXe: Charge gain & proportional scintillation on a single wire
Miyajima NIM 1976
Max gain ~100
Derenzo PR A 1974
Max gain ~400
LXe
LXe
LXe

## Slide 17: Electroluminescence on thin wires
Recent alpha-induced scintillation S1 and S2 electroluminescence signals recorded from a 10 micron diameter wire in LXe. Setup shown on left.
E. Aprile 2012, private communication
R&D in course

## Slide 18: Wires are delicate & gains are limited: Let’s play with electroluminescence in holes & photocathodes

## Slide 19: An Optical ion Gate
Grounded mesh blocks the ions
radiation
Scintillation light converted to photoelectrons on a CsI photocathode
Vhole
Xe 1 bar
Vhole [V]
Va-c = 220V
Va-c = 0 V
Radiation-induced electrons are multiplied in a first element
Avalanche-induced photons create photoelectrons on a CsI-coated multiplier
The photoelectrons continue the amplification process in the second element
No transfer of electrons or ions between elements: NO ION BACKFLOW
Avalanche-ions from first elements: blocked with a patterned electrode
For higher gains, the second element can be followed by additional ones
1st multiplier: constant gain
2ed multiplier: variable Vhole
MHSP
Aveiro/Coimbra/Weizmann
TPC Workshop LBL 2006
A. Breskin TPC2012 Paris Dec 2012

## Slide 20
Xenon: optical gain vs. pressure
Veloso, Amaro, dos Santos, Breskin, Lyashenko & Chechik. The Photon-Assisted Cascaded Electron Multiplier: a concept for potential avalanche-ion blocking 2006 JINST 1 P08003
An Optical ion Gate in Xe
IEEE TRANSACTIONS ON NUCLEAR SCIENCE, VOL. 56, NO. 3, JUNE 2009
Charge gain
Photon-induced
Charge gain
RESOLUTION MAINTAINED

## Slide 21: A cascaded Optical Gate
Higher optical gain
Amaro 2008

## Slide 22: Another optical gate… Budker
Optical gate in gas phase
Optical gate in 2-phase mode
Immersed electroluminescent GEM
Buzulutskov & Bondar, Electric and Photoelectric Gates for ion backflow suppression in multi-GEM structures. 2006 JINST 1 P08006

## Slide 23: The dream

## Slide 24: S1 & S2 recording with Liquid Hole-Multipliers LHM
Modest charge multiplication + Light-amplification in sensors immersed in the noble liquid, applied to the detection of both scintillation UV-photons (S1) and ionization electrons (S2).
UV-photons impinge on CsI-coated THGEM electrode;
extracted photoelectrons are trapped into the holes, where high fields induce electroluminescence (+possibly small charge gain);
resulting photons are further amplified by a cascade of CsI-coated THGEMs.
Similarly, drifting S2 electrons are focused into the hole and follow the same amplification path.
S1 and S2 signals are recorded optically by an immersed GPM or by charge collected on pads.
Holes:
Small- or no charge-gain
Electroluminescence (optical gain)
E
TPC Anode
S1 photon
Ionization electrons
Light or charge readout (GPM or pads)
CsI
Liquid xenon
E
E

## Slide 25: Staggered holes: blocking photon-feedback
L
S1 photon
S2 Ionization electrons
CsI
GPM
PADS
High light gain:
GPM readout
sufficient charge:
PAD readout
Feedback-photons from
final avalanche
or/and electroluminescence
BLOCKED by the cascade
Noble liquid

## Slide 26: S1 & S2 with LHM
A single-phase TPC DM detector with THGEM-LHMs.
The prompt S1 (scintillation) and the S2 (after ionization-electrons drift) signals are recorded with immersed CsI-coated cascaded-THGEMs at bottom and top.
Detects S1&S2
Detects S1

## Slide 27: S1 & S2 with LHM
Detects S1&S2
Detects S1&S2
A dual-sided single-phase TPC DM detector with top, bottom and side THGEM-LHMs.
The prompt S1 scintillation signals are detected with all LHMs. The S2 signals are recorded with bottom and top LHMs.
Highlights:
Higher S1 signals  lower expected detection threshold
Shorter drift lengths lower HV applied & lower e- losses

## Slide 28: CSCADED LHDs
L
E
LHM
LHM
LHM
LHM
LHM
S1, S2
S1
LOW HV for large-volume
Relaxed electron lifetime
Need: low radioactivity and pad-readout
C
C
C
C

## Slide 29: Summary & To-do list
A revived interest in single-phase Noble Liquid Detectors for large-volume systems.
A new concept proposed: scintillation & ionization recording with immersed Liquid Hole Multipliers – LHM
The dream needs validation:
THGEM charge & light Gain in LXe vs. hole-geometry
Electron collection efficiency into holes in LXe
Photon & electron yields in CsI-coated cascaded THGEM
Feedback suppression
S1/S2 Readout: pads vs. optical (GPM, others)
Radio-clean electrodes
We have a ready-to-go LXe-TPC system: WILiX
R&D proposal submitted

## Slide 30: spare

## Slide 31: Photoelectron extraction at low-T
Extraction efficiency (relative QE compared to vacuum) from CsI for 185nm UV photons as a function of the extraction field for pure CH4 and Ne/CH4(95:5) at 800 Torr in room- and LXe-temperatures.
CH4
175K
Ne/5%CH4 175K

## Slide 32: Weizmann Institute Liquid Xenon Facility (WILiX) TPC-GPM testing ground
Inner chamber (LXe)
Vacuum insulation
Gate valve
GPM load-lock
GPM guide, gas, cables
Xe heat exchanger
Xe liquefier
TPC
Basic consideration: allow frequent modifications in GPM without breaking the LXe equilibrium state
GPM

## Slide 33: APD/gAPD THGEM readout
Two-phase detector with a gAPD/WLS recording UV scintillation from a THGEM immersed in LAr.
Lightfoot JINST 2009
THGEM in LAr
Two-phase Ar detector with THGEM/gAPD optical readout in the NIR
Bondar, Buzulutskov JINST 2010
THGEMs in gas
Moneiro PL 2012
Photons/e @ 2 Bar Xe:
Parallel grids: ~400
GEM: ~1500
THGEM: ~8000